| Mineral sample | pH1 | R2,f (s-1) | [Cu] uM2 | [Fe] mM2 |
| --- | --- | --- | --- | --- |
| None |  | 1.4 | 0 | 0 |
| CJ08 | 7.77 | 4.6 | 0.031 | 3.31 |
| DT05 | 6.13 | 3.9 | 0.016 | 3.19 |
| BY073 | 4.35 | 644 | 0.173 | 0.11 |
| CB073 | 4.35 | 1750 | 0.394 | 11.22 |
| 1pH measurements were performed using a 1:10 dilution of the unbuffered leachate in deionized H2O. 2Metal ion concentrations were determined from ICP-OES analysis. 3NMR relaxation rate for mineral leachates were determined by extrapolation of data measured for diluted samples. |