Text S1. Morphology and size measurement

An optical microscope system (TE2000U, Nikon, USA) and a digital camera (Evolution color VF, Nikon, USA) were utilized to observe the collected microfibers morphology. The recorded pictures were further analyzed by a personal computer with the homemade images analysis software in MATLAB (MathWorks Inc., USA) to determine the average diameter of the microfibers. Scanning electron microscopy (SEM, Hitachi S-2700, Japan) was used to evaluate the surface morphology of the microfibers. All data were expressed as the mean ± standard deviation, and statistical analysis between studied groups was performed using ANOVA test.